## Slide 1: Mechanical Property Machine Learning Models
Robert Tang-Kong
Summary of Results

## Slide 2: Figure 1: Schematic ML Model Flow
Show data/information reduction pathway.
Identify what in/out is, what we have and what we want.
Identify where gaps used to be, or where Matminer fits in?
ability to produce large amounts of features quickly
Facilitates discussion of {dataset, features, and models}

## Slide 3: Figure A: All scatter plots for MG

## Slide 4: Table A: R2 for MG

## Slide 5: Generation definitions
gen-0: No changes to data, raw model.
gen-1: outliers removed, model retrained
gen-2: features reduced, model retrained
gen-3: vegards + diff, model trained on deviation from vegards
Retrain at each Generation

## Slide 6: Raw Data (generation 0)

## Slide 7: Data at gen-0 (before outlier removal)

## Slide 8: Removed outliers

## Slide 9: Methods for more mature ML models
Feature elimination/reduction
RFECV
Boosting using existing models
Notes: Both can be used to reveal which features are most important in a given model
For a less interpretable model, local importances can be extracted with something like LIME.

## Slide 10: Features, and what might be learned from them?

## Slide 11: CR with MG model

## Slide 12: Figure 3: Performance of ML on predicting density of amorphous glasses vs Vegard’s Law
Show efficacy of pre-existing theory?
Why is this so effective? Acting as essentially hard spheres?
Seeing a perfect (almost) gradation between close packing structures
Look at the features involved, they are understandably tied to things like radii
Learning where we deviate from the agreed theory is notably more effective
Is essentially highly weighting our prior understanding and focusing the model on deviations from it.4
Also can reveal what elemental properties are relevant for improvements in learning.
R2 Score | Gen. 0 | Gen. 1 | Gen. 2 | Gen. 3
RF | 0.841 | 0.934 | 0.937 | 0.974
Vegard’s | 0.861 | 0.930 | 0.930 | 0.930

## Slide 13: Figure 4: Performance of density predictions on MP dataset??
All Materials Project Data
(Trained on amorphous data) (Vegards law prediction) (Trained on MAPI data)
(Prediction of deviation from Vegards) (Prediction using deviation)
R2 Score | Gen. 0 | Gen. 1 | Gen. 2 | Gen. 3
RF | 0.875 | 0.916 | 0.925 | 0.970
Vegard’s | 0.792 | 0.848 | 0.848 | 0.848
Notes: Model trained on metallic glasses doesn’t do well, but this is very much to be expected.
What do features tell us? What’s different about this behavior?
Training on the crystalline dataset affords us some improvements, but not a huge amount.

## Slide 16: Initial models, density
Use density data as initial judge of model efficacy
  Random Forest, 12 feat/estimator
  Standard magpie features
  Removing single elements and problem compositions
  Thoughts
  Model not generalizing well, but good accuracy

## Slide 17: Initial models, density: Vegard’s law
Vegard’s law
We don’t beat the rule of mixtures quite yet…

## Slide 18: Feature Exploration: Density
Green  mode
Yellow  Mean
Purple  Minimum
Red  Maximum
Looking at density model features, ordered by importance
  Mode, mean trend to the top, while min/max seem less important  Could justifiably leave out min/max
  Near top, both mode and mean of same property appear together  may only need to choose one of mode/mean
These all come from cf.Stoichiometry(), which supplies 130 features…. Could cut down significantly

## Slide 19: Fitting model with reduced feature set
Use only mean ElementProperty features
  Not much of a change…
All 152 features

## Slide 20: Fitting model with reduced feature set
Using only mean
Standard features

## Slide 21: Outlier Data points
All highlighted compositions are:
Zr57 Nb5 Al10 Cu15.4 Ni12.6

## Slide 22: Outlier Data points: v2
Cu1.5Si1.5Ag0.3B4P18Pt74.7
Ta21Co11Ni18
Hf46Nb2Al13Cu29.25Ni9.75
Fe9P5Pt6

## Slide 23: Dropping GSvolume, Covalent Radius

## Slide 24: Model difference between real and Vegard’s law
Without outliers (same problem composition), r2 = 0.479
Without outliers the original model gives up to r2 = 0.913

## Slide 26: Training Default Model without problem composition

## Slide 27: Learning curve without outlier composition
Seems to perform as good if not better than Vegard’s law without those compositions
(R2 very sensitive to outliers)
Not much to learn/improve on here.

## Slide 28: Can we learn where Vegard’s law is lacking?
Features gathered over 5 training splits (used to make scatter plot)

## Slide 29: Investigating features used in models
Predicting Density
Predicting Density deviation from Vegard’s law
Notes: Training performed 5 times, top 5 from each instance collected.
Duplicate features (across separate training instances) have their importances summed to give a sort of averaged importance
Only melting Temperature in common

## Slide 30: Full Model vs Difference Model (pre rfecv)
Full Model | Importance | Rank in Diff Model
mode Number | 0.0605 | 38
mode AtomicWeight | 0.0603 | 39
mean NValence | 0.0566 | 36
mode NValence | 0.0538 | 7
mean Number | 0.0409 | 58
mean Electronegativity | 0.0304 | 19
mean AtomicWeight | 0.0302 | 61
mode Column | 0.0300 | 25
mode MeltingT | 0.0274 | 11
Difference Model | Importance | Rank in Full Model
avg_dev Column | 0.0330 | 86
minimum CovalentRadius | 0.0322 | 92
mean GSbandgap | 0.0294 | 34
avg_dev NpValence | 0.0257 | 35
avg_dev GSbandgap | 0.0251 | 23
mode NValence | 0.0233 | 5
minimum GSvolume_pa | 0.0218 | 93
mean GSmagmom | 0.0195 | 91
mean GSvolume_pa | 0.0191 | 57
Notes: Train on Vegards data exactly
Look up feats
Look at next few feats
Youngs mod
MP API To check and see other comps, see how model compares to DFT

## Slide 31: Vegards Model vs Difference Model
Difference Model | Importance | Rank in Full Model
avg_dev Column | 0.0330 | 86
minimum CovalentRadius | 0.0322 | 92
mean GSbandgap | 0.0294 | 34
avg_dev NpValence | 0.0257 | 35
avg_dev GSbandgap | 0.0251 | 23
mode NValence | 0.0233 | 5
minimum GSvolume_pa | 0.0218 | 93
mean GSmagmom | 0.0195 | 91
mean GSvolume_pa | 0.0191 | 57
Vegards Prediction Model | Importance | Rank in Diff Model
mode AtomicWeight | 0.0676 | 39
mean NValence | 0.0587 | 36
mode Number | 0.0522 | 38
avg d valence electrons | 0.0446 | 51
mode NValence | 0.0441 | 7
mean NdValence | 0.0440 | 48
mean Number | 0.0397 | 58
mean AtomicWeight | 0.0352 | 61
mean Electronegativity | 0.0279 | 19
Train model on vegards law predictions directly

## Slide 32: Looking at improvement on Vegard’s Law Predictions
(0.93  0.979, 5.04% improvement, 70% of available improvement)
r2 for difference predictions = 0.681
Notes: V+diff > full RF model > Vegards law.
Why doesn’t RF model do as well? It has all the same features…
What do we learn from physics

## Slide 33: Feature Importances
Notes: Our data is more monotonic, though not losing as much information as we might have initially expected.
For density it looks like we need far more than 12 features to capture say, 0.8 importance, and mean r2 performance tracks this (not getting close to 0.97 as we had before)

## Slide 34: Young’s Modulus performs worse with standard model
Youngs Model | Importance
mean GSvolume_pa | 0.0576
minimum CovalentRadius | 0.0478
mean MeltingT | 0.0457
minimum GSvolume_pa | 0.0448
mean Electronegativity | 0.0399
mode GSvolume_pa | 0.0346
maximum MeltingT | 0.0323
mean GSmagmom | 0.0317
mode GSmagmom | 0.0269
avg_dev GSbandgap | 0.0251
mode MeltingT | 0.0189
avg_dev GSmagmom | 0.0179
mode Electronegativity | 0.0173

## Slide 36: Materials Project Predictions (downsampled for speed)
Without 4 outliers: r2=0.9421

## Slide 37: Materials Project Predictions
Crystalline data not predicted well by model trained on amorphous data. (as expected)
Notes: Data is all materials project entries with density and <= 3 elements: ~50k data points
Taking only data within the same ternaries as own database: ~5k data points

## Slide 38: Vegard’s Law poorly predicts crystalline data

## Slide 39: Comparison to Vegards Law
Prediction of deviation from Vegard’s law is roughly as good as amorphous case (r2 = 0.681),
Performance of (Vegard’s + deviation prediction) does not improve as much (0.819  0.847, 3.4% improvement, 15.5% of available improvement)

## Slide 40: Materials Project Data
Crystalline Model | Importance
mean AtomicWeight | 0.0772
mean Number | 0.0688
mean MeltingT | 0.0558
mean NdValence | 0.0497
mean Row | 0.0461
avg d valence electrons | 0.0390
mode MendeleevNumber | 0.0339
mode MeltingT | 0.0335
mean Electronegativity | 0.0305
mean CovalentRadius | 0.0202
Full Model | Importance
mode Number | 0.0605
mode AtomicWeight | 0.0603
mean NValence | 0.0566
mode NValence | 0.0538
mean Number | 0.0409
mean Electronegativity | 0.0304
mean AtomicWeight | 0.0302
mode Column | 0.0300
mode MeltingT | 0.0274

## Slide 41: Outliers in MAPI data
Cu, Ta: one data point with extremely low density, 8 data points total (0.2 vs 8.8), (0.9 vs 15ish)
CeSe2: 45/176 abnormally low (2-3 vs 5-6)