## Slide 1: Mechanical Property Machine Learning Models
Robert Tang-Kong
Summary of Results

## Slide 2: Density Story: Failure
  How do models fail?
  Typographical errors
  Modeling / physics errors
    Can we beat simple models?
    Can we learn from the deviation from these simple models?
    Are we missing ensemble properties?

## Slide 3: Initial models, density
Use density data as initial judge of model efficacy
  Random Forest, 12 feat/estimator
  Standard magpie features
  Removing single elements and problem compositions
  Thoughts
  Model not generalizing well, but good accuracy

## Slide 4: Initial models, density: Vegard’s law
Vegard’s law
We don’t beat the rule of mixtures quite yet…

## Slide 5: Outlier Data points
All highlighted compositions are:
Zr57 Nb5 Al10 Cu15.4 Ni12.6

## Slide 6: Training Default Model without problem composition

## Slide 7: Can we learn where Vegard’s law is lacking?
Features gathered over 5 training splits (used to make scatter plot)

## Slide 8: Looking at improvement on Vegard’s Law Predictions
(Vegards + predicted difference)
Notes: V+diff > full RF model > Vegards law.
Why doesn’t RF model do as well? It has all the same features…
What do we learn from physics

## Slide 9: Full Model vs Difference Model
Full Model | Importance | Rank in Diff Model
mode Number | 0.0605 | 38
mode AtomicWeight | 0.0603 | 39
mean NValence | 0.0566 | 36
mode NValence | 0.0538 | 7
mean Number | 0.0409 | 58
mean Electronegativity | 0.0304 | 19
mean AtomicWeight | 0.0302 | 61
mode Column | 0.0300 | 25
mode MeltingT | 0.0274 | 11
Difference Model | Importance | Rank in Full Model
avg_dev Column | 0.0330 | 86
minimum CovalentRadius | 0.0322 | 92
mean GSbandgap | 0.0294 | 34
avg_dev NpValence | 0.0257 | 35
avg_dev GSbandgap | 0.0251 | 23
mode NValence | 0.0233 | 5
minimum GSvolume_pa | 0.0218 | 93
mean GSmagmom | 0.0195 | 91
mean GSvolume_pa | 0.0191 | 57
Notes: Train on Vegards data exactly
Look up feats
Look at next few feats
Youngs mod
MP API To check and see other comps, see how model compares to DFT

## Slide 10: Vegards Model vs Difference Model
Difference Model | Importance | Rank in Full Model
avg_dev Column | 0.0330 | 86
minimum CovalentRadius | 0.0322 | 92
mean GSbandgap | 0.0294 | 34
avg_dev NpValence | 0.0257 | 35
avg_dev GSbandgap | 0.0251 | 23
mode NValence | 0.0233 | 5
minimum GSvolume_pa | 0.0218 | 93
mean GSmagmom | 0.0195 | 91
mean GSvolume_pa | 0.0191 | 57
Vegards Prediction Model | Importance | Rank in Diff Model
mode AtomicWeight | 0.0676 | 39
mean NValence | 0.0587 | 36
mode Number | 0.0522 | 38
avg d valence electrons | 0.0446 | 51
mode NValence | 0.0441 | 7
mean NdValence | 0.0440 | 48
mean Number | 0.0397 | 58
mean AtomicWeight | 0.0352 | 61
mean Electronegativity | 0.0279 | 19
Train model on vegards law predictions directly

## Slide 11: Feature Importances
Notes: Our data is more monotonic, though not losing as much information as we might have initially expected.
For density it looks like we need far more than 12 features to capture say, 0.8 importance, and mean r2 performance tracks this (not getting close to 0.97 as we had before)