## Slide 1: Mechanical Property Machine Learning Models
Robert Tang-Kong
Summary of Results

## Slide 2: Initial models, density
Use density data as initial judge of model efficacy
  Random Forest, 12 feat/estimator
  Standard magpie features
  Removing single elements and problem compositions
  Thoughts
  Model not generalizing well, but good accuracy

## Slide 3: Initial models, density: Vegard’s law
Vegard’s law
We don’t beat the rule of mixtures quite yet…

## Slide 4: Feature Exploration: Density
Green  mode
Yellow  Mean
Purple  Minimum
Red  Maximum
Looking at density model features, ordered by importance
  Mode, mean trend to the top, while min/max seem less important  Could justifiably leave out min/max
  Near top, both mode and mean of same property appear together  may only need to choose one of mode/mean
These all come from cf.Stoichiometry(), which supplies 130 features…. Could cut down significantly

## Slide 5: Fitting model with reduced feature set
Use only mean ElementProperty features
  Not much of a change…
All 152 features

## Slide 6: Fitting model with reduced feature set
Using only mean
Standard features

## Slide 7: Outlier Data points
All highlighted compositions are:
Zr57 Nb5 Al10 Cu15.4 Ni12.6

## Slide 8: Dropping GSvolume, Covalent Radius

## Slide 9: Model difference between real and Vegard’s law
Without outliers (same problem composition), r2 = 0.479
Without outliers the original model gives up to r2 = 0.913

## Slide 11: Training Default Model without problem composition

## Slide 12: Learning curve without outlier composition
Seems to perform as good if not better than Vegard’s law without those compositions
(R2 very sensitive to outliers)
Not much to learn/improve on here.

## Slide 13: Can we learn where Vegard’s law is lacking?
Features gathered over 5 training splits (used to make scatter plot)

## Slide 14: Investigating features used in models
Predicting Density
Predicting Density deviation from Vegard’s law
Notes: Training performed 5 times, top 5 from each instance collected.
Duplicate features (across separate training instances) have their importances summed to give a sort of averaged importance
Only melting Temperature in common

## Slide 15: Full Model vs Difference Model
Full Model | Importance | Rank in Diff Model
mode Number | 0.0605 | 38
mode AtomicWeight | 0.0603 | 39
mean NValence | 0.0566 | 36
mode NValence | 0.0538 | 7
mean Number | 0.0409 | 58
mean Electronegativity | 0.0304 | 19
mean AtomicWeight | 0.0302 | 61
mode Column | 0.0300 | 25
mode MeltingT | 0.0274 | 11
Difference Model | Importance | Rank in Full Model
avg_dev Column | 0.0330 | 86
minimum CovalentRadius | 0.0322 | 92
mean GSbandgap | 0.0294 | 34
avg_dev NpValence | 0.0257 | 35
avg_dev GSbandgap | 0.0251 | 23
mode NValence | 0.0233 | 5
minimum GSvolume_pa | 0.0218 | 93
mean GSmagmom | 0.0195 | 91
mean GSvolume_pa | 0.0191 | 57
Notes: Train on Vegards data exactly
Look up feats
Look at next few feats
Youngs mod
MP API To check and see other comps, see how model compares to DFT

## Slide 16: Vegards Model vs Difference Model
Difference Model | Importance | Rank in Full Model
avg_dev Column | 0.0330 | 86
minimum CovalentRadius | 0.0322 | 92
mean GSbandgap | 0.0294 | 34
avg_dev NpValence | 0.0257 | 35
avg_dev GSbandgap | 0.0251 | 23
mode NValence | 0.0233 | 5
minimum GSvolume_pa | 0.0218 | 93
mean GSmagmom | 0.0195 | 91
mean GSvolume_pa | 0.0191 | 57
Vegards Prediction Model | Importance | Rank in Diff Model
mode AtomicWeight | 0.0676 | 39
mean NValence | 0.0587 | 36
mode Number | 0.0522 | 38
avg d valence electrons | 0.0446 | 51
mode NValence | 0.0441 | 7
mean NdValence | 0.0440 | 48
mean Number | 0.0397 | 58
mean AtomicWeight | 0.0352 | 61
mean Electronegativity | 0.0279 | 19
Train model on vegards law predictions directly

## Slide 17: Looking at improvement on Vegard’s Law Predictions
Notes: V+diff > full RF model > Vegards law.
Why doesn’t RF model do as well? It has all the same features…
What do we learn from physics

## Slide 18: Feature Importances
Notes: Our data is more monotonic, though not losing as much information as we might have initially expected.
For density it looks like we need far more than 12 features to capture say, 0.8 importance, and mean r2 performance tracks this (not getting close to 0.97 as we had before)

## Slide 19: Young’s Modulus performs worse with standard model
Youngs Model | Importance
mean GSvolume_pa | 0.0576
minimum CovalentRadius | 0.0478
mean MeltingT | 0.0457
minimum GSvolume_pa | 0.0448
mean Electronegativity | 0.0399
mode GSvolume_pa | 0.0346
maximum MeltingT | 0.0323
mean GSmagmom | 0.0317
mode GSmagmom | 0.0269
avg_dev GSbandgap | 0.0251
mode MeltingT | 0.0189
avg_dev GSmagmom | 0.0179
mode Electronegativity | 0.0173

## Slide 21: Materials Project Predictions
Without 4 outliers: r2=0.9421

## Slide 22: Materials Project Data
Crystalline Model | Importance
mean AtomicWeight | 0.0772
mean Number | 0.0688
mean MeltingT | 0.0558
mean NdValence | 0.0497
mean Row | 0.0461
avg d valence electrons | 0.0390
mode MendeleevNumber | 0.0339
mode MeltingT | 0.0335
mean Electronegativity | 0.0305
mean CovalentRadius | 0.0202
Full Model | Importance
mode Number | 0.0605
mode AtomicWeight | 0.0603
mean NValence | 0.0566
mode NValence | 0.0538
mean Number | 0.0409
mean Electronegativity | 0.0304
mean AtomicWeight | 0.0302
mode Column | 0.0300
mode MeltingT | 0.0274